RCA CLEANING PROCESS

(SC-1, Oxide, SC-2)

The cleaning steps outlined below must be followed consecutively in order to achieve the best results.  You should prepare all baths prior to starting the cleaning process.

- STANDARD CLEAN No.1(SC-1)

  - Chemicals and mixing ratio

    - 5 parts Di water

    - 1 part Ammonium Hydroxide (NH4OH – 28%)

    - 1 part Hydrogen Peroxide (H2O2 – 30%)

  - Equipment/Apparatus

    - Wet bench

      - chemical tank #4 (unless heated solution is desired)

    - Wafer(s) holder

    - Beaker (optional)

  - Process

    - Add 100ml of ammonium hydroxide to tank #4

    - Add 100ml of hydrogen peroxide to tank #4

    - Add 500ml of DI water to tank #4.

    - Place wafer(s) into tank and hold for 5 minutes or until metals have been removed.

    - Rinse with DI water tank #2 for 3 minutes while flushing tank.

    - Immediately place wafers into HF bath for the oxide clean.

Note: If heated bath is desired, submerge wafers in holder with wafers in cold solution and place the beaker on hot plate.

- Heat solution to 75 to 80°C and maintain temp.

- Place wafer(s) into solution and hold for 5 minutes or until metals have been removed.

- Remove wafer(s) and place it immediately in DI water tank #2

and rinse for 3 minutes while flushing tank.

4.  Transfer wafer(s) directly into oxide clean bath.

  - Clean-up

    - Use the chemical aspirator to dispose of chemical waste after solution has cooled down.

    - Rinse out chemical tank with DI water and aspirate to remove rinsing water.

    - Rinse, dry and put away all chemical mixing containers.

    - Wipe down all working surfaces on wet bench.

    - Turn off air and DI water supply to wet bench.

- OXIDE CLEAN

  - Chemicals and mixing ratio

    - 1 part Hydrofluoric Acid (HF – 49%)

    - 30 parts DI water

  - Equipment/Apparatus

    - Propylene beaker (DO NOT use glass beaker for HF chemical processing)

    - Wafer(s) holder

  - Process

    - Pour DI water into beaker.

    - Pour acid into beaker and mix.

    - Place wafer(s) into solution for 15 seconds. Exposed silicon (but not SiO2) should repel HF solution.

    - Rinse in DI water tank #2 for 30 seconds to remove HF solution (this minimizes re-growth of a hydrous oxide film).

    - Transfer wafer assembly immediately, without drying, into hot SC - 2 solution.

- STANDARD CLEAN No.2(SC-2) – desorption of ionic and heavy metal atomic contaminants

  - Chemicals needed and mixing ratio

    - 6 parts DI water

    - 1 part Hydrogen Peroxide (H2O2 – 30%)

    - 1 part Hydrochloric Acid (HCL – 37%)

  - Equipment/Apparatus

    - Wet bench

      - use chemical tank #6

      - wafer holder

      - beaker (optional)

  - Process

    - Pour chemicals into chemical tank.  Be sure to add acid to water and not vice versa.

    - Submerge wet wafers from HF clean into bath for 10 minutes or until metals have been dissolved.

    - Remove wafers from bath and immediately place wafers in dirty DI rinse tank #2 while flushing tank for 5 minutes.

    - Rinse wafers in clean DI rinse tank #8 for 30 seconds.

    - Dry wafers with N2 gun.

Note: If heated bath is desired, submerge wafers in holder with wafers in cold solution and place the beaker on hot plate.

      - Heat solution to 75 to 80°C and maintain temp.

      - Place wafer(s) into solution and hold for 10 minutes or until metals have been disolved.

      - Remove wafer(s) and place it immediately in DI water tank #2

      - and rinse for 5 minutes while flushing tank.

      - Rinse wafers with clean DI rinse tank #8 for 30 seconds.

      - Dry with N2 gun.

  - Clean-up

    - Use the chemical aspirator to dispose of chemical waste after solution has cooled down.

    - Rinse out chemical tank with DI water and aspirate to remove rinsing water.

    - Rinse, dry and put away all chemical mixing containers.

    - Wipe down all working surfaces on wet bench.

    - Turn off air and DI water supply to wet bench.